Synthesis, characterization, and theoretical study of new cocrystals and charge-transfer compounds

Zarife Sibel ŞAHİN1,*, Zeki KARTAL2

1Department of Energy Systems Engineering, Faculty of Engineering and Architecture, Sinop University, Sinop, Turkiye

2Retired Professor of Atomic and Molecular Physics, Kütahya Dumlupınar University, Kütahya, Turkiye

* Correspondence: zarifesibel@sinop.edu.tr

Zarife Sibel ŞAHİN: https://orcid.org/ 0000-0003-2745-7871

Zeki KARTAL: https://orcid.org/0000-0001-9739-0858

Supplementary materials

Figure S1. A portion of the crystal structure of compound 1 showing the formation of R44(16) rings edge fused along [111].

Figure S2. A portion of the crystal structure of compound 2 illustrating the formation of chain edge-fused R86(28) and R44(20) rings.

Figure S3. An infinite 3D supramolecular network.

Figure S4. 2D fingerprint plots were generated to illustrate these interactions based on surface projections of compounds 1–3.

Figure S5. 3D views of the voids formed depending on the electron arrangement in the structure for (a) compound 1, (b) compound 2, and (c) compound 3.

Figure S6. Energy values of the components of the total interaction energies of compounds 1–3. In the tables, N denotes the number of molecular pairs interacting with the reference molecule, Symop refers to the symmetry operations applied to the reference molecule, R indicates the distance (in Å) between the center of mass of the reference molecule and those of its neighboring molecules, and E represents the individual components of the calculated interaction energies.

Figure S7. The charge distribution graphs of the UV transitions with the highest Ci coefficients of compounds 1, 2 and 3.

Table S1. Elemental analysis data for the compounds.

| Compounds; Mr (g) | Elemental analysis, (calculated) (%)/found (%) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | C | H | N | S | Ni |
| [(C8H14O4)(C6H4N2)2]; 382.41 | (62.82) 62.79 | (5.80) 5.83 | (14.65) 14.71 | (-) - | (-) - |
| [(C5H7N2)+·(NCS)-]; 153.20 | (47.04) 46.96 | (4.61) 4.64 | (27.43) 27.51 | (20.93) 20.98 | (-) - |
| [Ni(CN)4.2(C5H7N2).2(H2O)]; 389.04 | (43.22) 43.08 | (4.66) 4.61 | (28.80) 28.91 | (-) - | (15.09) 15.12 |

Table S2. Crystallographic data of compounds 1-3.

| Crystal data | 1 | 2 | 3 |
| --- | --- | --- | --- |
| Empirical formula | C20H22N4O4 | C6H7N3S | C14H18N8O2Ni |
| Formula weight | 382.41 | 153.21 | 389.07 |
| Crystal system | Triclinic | Monoclinic | Monoclinic |
| Space group | P1 | P21/n | C2/m |
| a (Å) | 6.3263 (6) | 5.0581 (5) | 10.4345 (13) |
| b (Å) | 8.5643 (8) | 17.3940 (17) | 12.6008 (16) |
| c (Å) | 9.5987 (10) | 8.6270 (8) | 7.3076 (10) |
|  (º) | 79.856 (4) | 90.000 | 90.000 |
|  (º) | 79.921 (5) | 95.412 (3) | 108.091 (5) |
|  (º) | 83.893 (4) | 90.000 | 90.000 |
| V (Å3) | 502.50 (9) | 755.63 (13) | 913.3 (2) |
| Z | 1 | 4 | 2 |
| Dc (g cm-3) | 1.264 | 1.347 | 1.415 |
| μ (mm-1) | 0.09 | 0.35 | 1.09 |
| θ range (º) | 3.0–28.0 | 2.3–26.9 | 2.6–28.4 |
| Measured refls. | 26630 | 20758 | 8070 |
| Independent refls. | 2422 | 1609 | 1200 |
| Rint | 0.063 | 0.028 | 0.050 |
| S | 1.07 | 1.10 | 1.08 |
| R1/wR2 | 0.052/0.159 | 0.033/0.076 | 0.036/0.079 |
| Tmax/Tmin | 0.642/0.746 | 0.667/0.745 | 0.437, 0.746 |
| CCDC | 2334512 | 2334585 | 2374519 |

Table S3. Vibration frequencies in the free states of the ligands used in the preparation of compounds and in the compounds.

| Assignment | 4CP a | SA b | 1 | 4AP c | KSCNd | 2 | 4AP c | K2Ni(CN)4·H2O d | 3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ν(O-H) Free H2O | - | - | - | - | - | - | - | - | 3604 w |
| νas(O-H) water | - | - | - | - | - | - | - | 3469 w | - |
| νs(O-H) water | - | - | - | - | - | - | - | 3245 w | - |
| ν(O-H) carboxy. | - | 3416 w | 2668 w | - | - | - | - | - | - |
| νas(NH2) | - | - | - | 3430 s | - | 3458 s | 3430 s | - | 3384 w |
| ν(N-H) | - | - | - | - | - | 3437 s | - | - | 3334 s |
| νs(NH2) | - | - | - | 3303 w | - | 3349 s | 3303 w | - | 3235 m |
| ν(C-H) aromatic | 3089 w | - | 3153 w 3113 w | 3100 w | - | 3219 m | 3100 w | - | 3160 m |
| ν(C-H) aromatic | 3023 w | - | 3088 m 3041 w | 3079 w | - | 3068 w | 3079 w | - | 3053 m |
| ν(C-H) aliphatic | - | 2943 s | 2943 s | - | - | - | - | - | - |
| ν(COH) | - | 2869 m | 2866 w | - | - | - | - | - | - |
| δ(O-H) carboxylic | - | 2530 w | 2765 w | - | - | - | - | - | - |
| ν(C≡N) | 2235 m | - | 2240 m | - | 2036 s | 2104 s 2071 s 2023 w | - | 2121 s | 2123 s |
| ν(C=O) carboxy. | - | 1683 s | 1709 s | - | - | - | - | - | - |
| δ(OH) water | - | - | - | - | - | - | - | 1652 s | 1650 s |
| δ(NH2) | - | - | - | 1649 m | - | 1685 w | 1649 m | - | 1673 s |
| ν(C=C) | 1588 m | - | 1600 s | 1585 s | - | 1624 s | 1585 s | - | 1650 s |
| ν(C-C) | 1541 m |  | 1547 m | 1429 w | - | 1449 m | 1429 w | - | 1402 m |
| ν(C-N) | 1486 m | - | 1499 m | 1267 m | - | 1280 m | 1267 m | - | 1241 w |
| δ(CH2) | - | 1466 w | 1465 w | - | - | - | - | - | - |
| ν(C-N) | 1413 m | - | 1410 s | - | - | - | - | - | - |
| δ(C=O) carboxy., δ(HCH) | - | 1332 s 1254 s 1190 s | 1332 s 1240 s 1179 s | - | - | - | - | - | - |
| νring (2.) | 1079 m | - | 1071w | - | - | - |  | - | - |
| ω(CH2), δ(C-O) | - | 1059w | 1064 s | - | - | - | - | - | - |
| νring (1.) | 982 m | - | 1007 s | 976 s | - | 1013 s | 976 s | - | 997 s |
| ν(C-S) | - | - | - | - | 740 m | 824 s | - | - | - |
| ν(Ni-CN) | - | - | - | - | - | - | - | 544 w | 530 w |
| δ(NCS) | - | - | - | - | 474 s | 529 s | - | - | - |
| π(Ni-CN) | - | - | - | - | - | - | - | 442 w | 496 s |
| δ(Ni-CN) | - | - | - | - | - | - | - | 420 w | 414 s |

ν: stretching; δ: in plane bending; π: out of plane bending; ω: wagging; s: strong; m: medium; w: weak; a taken from Macrae et al. [36], b taken from Kartal and Şahin [21].

Table S4. Mulliken electric charges of the atoms in compounds 1–3 and their values ​​in terms of free electron charge (e).

| Compound 1 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Atom | ACVFL | ACVC | Atom | ACVFL | ACVC | Atom | ACVFL | ACVC |
| C1 | 0.185957 | 0.099877 | H9A | 0.142383 | 0.171837 | H10B | 0.141712 | 0.159087 |
| H1 | 0.023729 | 0.198678 | H9B | 0.15869 | 0.191049 | O1i | -0.30536 | -0.42514 |
| C2 | -0.1224 | -0.16006 | C10 | -0.23221 | -0.33283 | O2i | -0.21499 | -0.56903 |
| H2 | 0.060696 | 0.203404 | H10A | 0.140167 | 0.160398 | H2Ai | 0.26926 | 0.41346 |
| C3 | 0.212041 | 0.125705 | H10B | 0.135592 | 0.173881 | C5i | 0.18596 | 0.09995 |
| C4 | -0.12165 | -0.1438 | O1 | -0.25318 | -0.42502 | H5i | 0.023729 | 0.19919 |
| H4 | 0.074322 | 0.206395 | O2 | -0.1496 | -0.56927 | C4i | -0.1224 | -0.15988 |
| C5 | 0.192347 | 0.079094 | H2A | 0.240284 | 0.413334 | H4i | 0.060696 | 0.203937 |
| H5 | 0.038906 | 0.248688 | C7 | 0.036922 | 0.521698 | C3i | 0.212041 | 0.125701 |
| C6 | 0.136608 | -0.21773 | C8 | -0.14066 | -0.46139 | C6i | -0.12165 | -0.14398 |
| N1 | -0.36829 | -0.5239 | H8A | 0.187923 | 0.207189 | H2i | 0.074322 | 0.20588 |
| N2 | -0.31227 | -0.0685 | H8B | 0.169527 | 0.21938 | C2i | 0.192347 | 0.07899 |
| C7 | -0.46826 | 0.521449 | C9 | -0.35082 | -0.31916 | H1i | 0.038906 | 0.248284 |
| C8 | -0.32338 | -0.46108 | H9A | 0.154158 | 0.186726 | C1i | 0.136608 | -0.21773 |
| H8A | 0.183773 | 0.221749 | H9B | 0.164792 | 0.178489 | N1i | -0.36829 | -0.52395 |
| H8B | 0.160461 | 0.206576 | C10 | -0.27269 | -0.33276 | N2i | -0.31227 | -0.06852 |
| C9 | -0.04779 | -0.31918 | H10A | 0.14608 | 0.172796 |  |  |  |
| Symmetry code: (i) -x, 2-y, 2-z |  |  |  |  |  |  |  |  |
| Compound 2 |  |  |  |  |  |  |  |  |
| Atom | ACVFL | ACVC | Atom | ACVFL | ACVC | Atom | ACVFL | ACVC |
| C1 | -0.339235 | 0.182705 | H4 | 0.107513 | 0.267343 | H2A | 0.233609 | 0.356867 |
| H1 | 0.129635 | 0.240808 | C5 | -0.339235 | 0.190058 | H2B | 0.233609 | 0.387064 |
| C2 | 0.253458 | -0.29816 | H5 | 0.129635 | 0.247489 | C6 | 0.096503 | -0.23122 |
| H2 | 0.107513 | 0.237178 | N1 | -0.112994 | -0.67646 | S1 | 0.107499 | -0.23649 |
| C3 | -0.293325 | 0.422293 | H1A | - | 0.358431 | N3 | -0.204003 | -0.39235 |
| C4 | 0.253458 | -0.25616 | N2 | -0.363642 | -0.7994 |  |  |  |
| Compound 3 |  |  |  |  |  |  |  |  |
| Atom | ACVFL | ACVC | Atom | ACVFL | ACVC | Atom | ACVFL | ACVC |
| C1 | 0,310923 | 0,267627 | Ni1 | 2,183421 | -0,090983 | H1ii | 0.015475 | 0.180884 |
| H1 | 0,015475 | 0,107014 | C4 | -0,707764 | 0,300629 | C2ii | -0.254572 | -0.291715 |
| C2 | -0,254572 | -0,2859 | N3iv | -0,337463 | -0,591525 | H2ii | 0.029941 | 0.134226 |
| H2 | 0,029941 | 0,083524 | C4iv | -0,708138 | 0,116542 | C3ii | 0.657298 | 0.82504 |
| C3 | 0,657298 | 0,823835 | N3v | -0,337221 | -0,67594 | N2ii | -0.704055 | -0.769413 |
| N2 | -0,704055 | -0,734464 | C4v | -0,709188 | 0,212215 | H3ii | 0.199996 | 0.356279 |
| H3A | 0,199996 | 0,255071 | N3iii | -0,337316 | -0,702929 | N1ii | -0.556768 | -0.442579 |
| N1 | -0,556768 | -0,414606 | C4iii | -0,708784 | 0,204251 | H1Aii | 0 | 0.273931 |
| H1A | 0 | 0,28208 | O1 | -0,714341 | -0,726339 | C1iii | 0.310923 | 0.268312 |
| C1i | 0,310923 | 0,336997 | H4 | 0,357171 | 0,317839 | H1iii | 0.015475 | 0.103998 |
| H1i | 0,015475 | 0,182776 | H4i | 0,357171 | 0,395203 | C2iii | -0.254572 | -0.29349 |
| C2i | -0,254572 | -0,288087 | O1v | -0.714341 | -0.766539 | H2iii | 0.029941 | 0.082008 |
| H2i | 0,029941 | 0,135542 | H4v | 0.357171 | 0.320312 | H3iii | 0.199996 | 0.252242 |
| H3i | 0,199996 | 0,28019 | H4ii | 0.357171 | 0.320312 |  |  |  |
| N3 | -0,337546 | -0,795252 | C1ii | 0.310923 | 0.341625 |  |  |  |
| Symmetry codes: (i) x, −y+1, z; (ii) x, y+1, z; (iii) x, −y+2, z; (iv) 1−x, y, −z+2; (v) 1−x, −y+2, −z+2 |  |  |  |  |  |  |  |  |

ACVFL: atomic charge value in free ligand, ACVC: atomic charge value in the compound.

Table S5. General properties of voids in unit cells of compounds 1–3.

| Compounds | Volume (Å³) | RVVTV (%) | Void area (Å²) | Globularity | Asphericity |
| --- | --- | --- | --- | --- | --- |
| 1 | 51.57 | 10.26 | 209.23 | 0.320 | 0.071 |
| 2 | 62.01 | 08.21 | 283.34 | 0.267 | 0.363 |
| 3 | 101.62 | 11.13 | 399.12 | 0.264 | 0.094 |

RVVTV (%): ratio of void volume to total volume (%).

Table S6. Theoretically calculated absorption wavelength (λ), excitation energy values, ​​​​and oscillator strengths (f) for electronic transitions in the UV–visible region of compounds 1–3 in water.

| Compounds | Exc. States | Exc. energy (eV) | W. length (nm) | Osc. strengths | Assignments |  | Coefficients Ci |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | From → to |  |  |
| 1 | 1 | 4.5752 | 270.99 | 0.0022 | 101 →102 |  | 0.35297 |
|  | 2 | 5.0403 | 245.99 | 0.0537 | 99 →102 |  | 0.42547 |
| 2 | 1 | 5.2943 | 234.18 | 0.0311 | 40 → 43 | 0.60991 |  |
|  | 2 | 5.2998 | 233.94 | 0.0365 | 39 → 43 | 0.60626 |  |
|  | 3 | 5.3711 | 230.83 | 0.3522 | 38 → 41 | 0.60937 |  |
|  | 4 | 5.9019 | 210.07 | 0.0065 | 40 → 48 | 0.30511 |  |
|  | 5 | 5.9284 | 209.14 | 0.0153 | 39 → 44 | 0.44050 |  |
|  | 6 | 5.9374 | 208.82 | 0.0094 | 40 → 44 | 0.36001 |  |
|  | 7 | 6.2667 | 197.84 | 0.2529 | 37 → 41 | 0.61766 |  |
|  | 8 | 6.3377 | 195.63 | 0.0783 | 39 → 45 | 0.44512 |  |
|  | 9 | 6.3555 | 195.08 | 0.0099 | 40 → 46 | 0.43463 |  |
|  | 10 | 6.4032 | 193.63 | 0.1327 | 39 → 46 | 0.40721 |  |
|  | 11 | 6.6465 | 186.54 | 0.1281 | 39 → 48 | 0.33577 |  |
| 3 | 1 | 3.8337 | 323.40 | 0.0046 | 96 →100 | 0.63710 |  |
|  | 2 | 4.4894 | 276.17 | 0.0018 | 95 →100 | 0.53491 |  |
|  | 3 | 4.5040 | 275.28 | 0.0010 | 95 →101 | 0.61746 |  |
|  | 4 | 4.5855 | 270.38 | 0.0010 | 94 → 98 | 0.69440 |  |
|  | 5 | 4.6296 | 267.81 | 0.0010 | 91 → 97 | 0.62552 |  |

Table S7. The NMR theoretical isotropic and anisotropic chemical and magnetic shielding values calculated for compounds 1–3 in water at room temperature.

| Atoms | Degeneracy | Chemical and Magnetic shielding values (ppm) |  |  | Atoms |  | Degeneracy |  | Chemical and Magnetic shielding values (ppm) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Isotropic |  | Anisotropic |  |  |  |  | Isotropic |  |  | Anisotropic |  |
|  |  | Average | Shielding value corrected to TMS |  |  |  |  |  | Average | Shielding value corrected to TMS |  |  |  |
| Compound 1 |  |  |  |  |  | Compound 3 |  |  |  |  |  |  |  |
| N1; N1i | 2 | -77.4686 | - | 582.0642; 582.0335 | Ni1 |  | 1 |  | -2586.7388 | - |  | 1827.9694 |  |
| O1i; O1 | 2 | -55.5268 | - | 548.0302; 547.9990 | N3iv |  | 1 |  | 18.4187 | - |  | 404.4922 |  |
| N2i; N2 | 2 | -20.9669 | - | 404.8143; 404.8767 | N3iii |  | 1 |  | 19.0846 | - |  | 404.1132 |  |
| C7i; C7 | 2 | 2.5300 | 179.9356 | 110.6551; 110.6303 | H1A; H1; H1i |  | 3 |  | 27.0021 | 4.8800 |  | 10.5859; 3.8035; 3.7475 |  |
| H1i; H5 | 2 | 24.8471 | 7.0350 | 12.6492; 12.6487 | H1ii; H2 |  | 2 |  | 27.0939 | 4.7882 |  | 4.5607; 5.3910 |  |
| 40; 2 | 2 | 25.0739 | 6.8082 | 10.9427; 10.9453 | H1Aii |  | 1 |  | 27.1650 | 4.7171 |  | 11.3373 |  |
| H2i; H4 | 2 | 26.4604 | 5.4218 | 10.4524; 10.4497 | N3v |  | 1 |  | 27.2534 | - |  | 394.4694 |  |
| H4i; H2; H2Ai; H2A | 4 | 26.5820 | 5.3001 | 9.6859; 9.6866; 25.7544; 25.7555 | N3 |  | 1 |  | 27.3236 | - |  | 394.5214 |  |
| C1; C5i | 2 | 31.8678 | 150.5979 | 205.1792; 205.1587 | H2i; C2ii |  | 2 |  | 27.8204 | 4.0617 |  | 5.6677; 5.4956 |  |
| C2i; C5 | 2 | 32.7743 | 149.6913 | 208.3641; 208.3544 | H2 |  | 1 |  | 28.0483 | 3.8338 |  | 5.3910 |  |
| H8Ai; H8A | 2 | 33.5398 | -1.6577 | 6.4264; 6.4265 | H2iii |  | 1 |  | 28.1013 | 3.7808 |  | 5.7788 |  |
| H8Bi; H8B | 2 | 33.6326 | -1.7505 | 6.8397; 6.8402 | H3ii |  | 1 |  | 29.9086 | 1.9735 |  | 23.0404 |  |
| H9Ai; H9A; H9Bi; H9B | 4 | 34.7525 | -2.8704 | 6.5594; 6.5588; 6.4658; 6.4662 | H3iii |  | 1 |  | 30.8971 | 0.9850 |  | 16.0191 |  |
| H10Bi; H10B; H10Ai; H10A | 4 | 35.0636 | -3.1815 | 5.6887; 5.6887; 5.8884; 5.8883 | H3 |  | 1 |  | 30.9689 | 0.9132 |  | 17.3244 |  |
| C6i; C4; C4i; C2 | 4 | 57.0092 | 125.4565 | 205.0740; 205.0513; 204.6876; 204.6891 | H3i |  | 1 |  | 31.0493 | 0.8328 |  | 16.3431 |  |
| C3i; C3 | 2 | 57.8151 | 124.6505 | 166.5969; 166.5523 | H4ii |  | 1 |  | 39.8542 | -7.9721 |  | 33.1446 |  |
| C6; C1i | 2 | 59.9681 | 122.4975 | 343.5704; 343.5635 | H4i |  | 1 |  | 40.5973 | -8.7152 |  | 32.6554 |  |
| O2i; O2 | 2 | 136.5687 | - | 150.3062; 150.3564 | H4v |  | 1 |  | 40.7827 | -8.9006 |  | 27.4667 |  |
| C8i; C8 | 2 | 163.2417 | 19.2239 | 60.3515; 60.3550 | H4 |  | 1 |  | 41.6419 | -9.7598 |  | 27.7890 |  |
| C10i; C10 | 2 | 174.4890 | 7.9767 | 40.3303; 40.3291 | C3ii; C3 |  | 2 |  | 111.2826 | 71.1830 |  | 145.0106; 144.8900 |  |
| C9i; C9 | 2 | 177.9147 | 4.5510 | 34.1464; 34.1461 | C1i |  | 1 |  | 123.3134 | 59.1522 |  | 132.0055 |  |
| Compound 2 |  |  |  |  |  | C1ii |  | 1 | 123.5421 |  | 58.9235 |  | 130.9552 |
| C3 | 1 | 20.1622 | 162.3034 | 212.9816 | C1 |  | 1 |  | 123.6703 | 58.7953 |  | 131.0293 |  |
| H1A | 1 | 26.2784 | 5.6037 | 5.2996 | C1iii |  | 1 |  | 124.0354 | 58.4302 |  | 130.5657 |  |
| H1 | 1 | 26.4928 | 5.3893 | 6.7229 | C2iii |  | 1 |  | 140.5114 | 41.9542 |  | 130.1068 |  |
| H5 | 1 | 26.5561 | 5.3260 | 6.9611 | C2 |  | 1 |  | 140.5915 | 41.8741 |  | 130.8112 |  |
| H2 | 1 | 27.6679 | 4.2142 | 8.1085 | C2i |  | 1 |  | 141.1750 | 41.2906 |  | 129.6856 |  |
| H3 | 1 | 27.8076 | 4.0745 | 8.4217 | C2ii |  | 1 |  | 141.4054 | 41.0602 |  | 128.8266 |  |
| H2B | 1 | 31.5921 | 0.2900 | 19.5286 | C4 |  | 1 |  | 157.2165 | 25.2491 |  | 195.3953 |  |
| H2A | 1 | 32.5481 | -0.6660 | 8.8607 | C4v |  | 1 |  | 157.8921 | 24.5735 |  | 194.5823 |  |
| N3 | 1 | 40.9136 | - | 461.3638 | C4iii |  | 1 |  | 160.6767 | 21.7889 |  | 190.2298 |  |
| C1 | 1 | 44.8297 | 137.6359 | 188.5759 | C4iv |  | 1 |  | 161.6263 | 20.8393 |  | 188.7025 |  |
| C5 | 1 | 46.2372 | 136.2284 | 187.5499 | N1 |  | 1 |  | 207.9435 | - |  | 142.1206 |  |
| C6 | 1 | 46.6949 | 135.7707 | 367.2538 | N1ii |  | 1 |  | 208.9679 | - |  | 140.1005 |  |
| C2 | 1 | 75.5923 | 106.8733 | 164.1584 | N2ii |  | 1 |  | 253.0385 | - |  | 40.2423 |  |
| C3 | 1 | 76.1971 | 106.2685 | 164.6129 | N2 |  | 1 |  | 255.5806 | - |  | 35.4744 |  |
| N1 | 1 | 101.1524 | - | 227.4076 | O1 |  | 1 |  | 431.0153 | - |  | 19.1125 |  |
| N2 | 1 | 179.3116 | - | 65.2685 | O1v |  | 1 |  | 433.2705 | - |  | 19.5665 |  |
| S1 | 1 | 800.4815 | - | 393.7182 |  |  |  |  |  |  |  |  |  |